TENGIZCHEVRIOL /ТЕНГИЗШЕВРОЙЛ

PROJECT TITLE:                             K3 WASTE WATER UPGRADE

НАЗВАНИЕ ПРОЕКТА:   МОДЕРНИЗАЦИЯ СИСТЕМЫ СТОЧНЫХ ВОД К-3

PROJECT NUMBER / НОМЕР ПРОЕКТА:                                     X-062-056-08

AFE NUMBER / НОМЕР РОЗ:                                                           9410110405

DOCUMENT TITLE:                                    METOD STATEMENT FOR PIPING FABRICATION & INSTALLATION

НАЗВАНИЕ ДОКУМЕНТА :   ПЛАН ПРОИЗВОДСТВЕННЫХ РАБОТ ПО  ИЗГОТОВЛЕНИЮ И МОНТАЖУ ТРУБ

DOCUMENT NUMBER / НОМЕР ДОКУМЕНТА:                           PRO

CONTRACTOR / ПОДРЯДЧИК:

SUPPLIER /ПОСТАВЩИК:

PURCHASE ORDER (PO) /  ЗАКАЗ НА ПОКУПКУ

SUPPLIER DOCUMENT NUMBER /

НОМЕР ДОКУМЕНТА ПОСТАВЩИКА                                    SICIM S.P.A.

SUPPLIER DOCUMENT REVISION /

НОМЕР РЕДАКЦИИ ПОСТАВЩИКА

THIS IS A CONTROLLED DOCUMENT NO UN-AUTHORISED MODIFICATIONS  /  ДАННЫЙ ДОКУМЕНТ ЯВЛЯЕТСЯ КОНТРОЛИРУЕМЫМ. НЕ ВНОСИТЬ НЕ УТВЕРЖДЕННЫХ ИЗМЕНЕНИЙ

THIS DOCUMENT IS DUAL LANGUAGE. ENSURE BOTH  VERSION ARE MODIFIED

ДАННЫЙ ДОКУМЕНТ ВЫПОЛНЕН  НА ДВУХ ЯЗЫКАХ. УБЕДИТЕСЬ, ЧТО ИЗМЕНЕНИЯ ВНЕСЕНЫ В ОБУ ВЕРСИИ

| A | 30-09-2012 | IFRC | GCD | MC | NDN | CAI | CAI | CAI | CAI |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| REV/ РЕД | DATE/ ДАТА | STATE CODE/ СТАТУС | BY/ ПОДГ | CHK/ ПРОВ | APP/ УТВ | PROJ / ПРОЕКТ | CONST/ СТРОИТ.ОТДЕЛ | MAINT / ТЕХ.ОБСЛ | OPS/ПРО-ИЗВ.ОТД. |
| REVISIONS/ РЕДАКЦИИ | PROJECT APPROVAL / ДОКУМЕНТ УТВЕРЖДЕН ПРОЕКТОМ | TCJ APPROVALS ДОКУМЕНТ УТВЕРЖДЕН ТШО |

REVISION DESCRIPTION SHEET / ПЕРЕЧЕНЬ РЕДАКЦИЙ

| REV./ РЕВ. | PARA./ ПАРАГ. | REVISION DESCRIPTION / ОПИСАНИЕ РЕДАКЦИЙ |
| --- | --- | --- |
| A |  | Issuer for review and comments/ Выпущено для рассмотрения и комментариев |

Страница подписей:                                                                                  Signature Page:

Утверждено:                                                                                        Approved:

(Должность)____________________________________________ (Position):

Nicola Di Nicola / Никола Ди Никола

Sicim Project Manager / Менеджер по проектам ,Сичим

Проверено/Одобрено                                                       Reviewed / Endorsed

(Должность)____________________________________________ (Position):

Leo Mirti / Лео Мирти

Sicim Constractor Manager /

Менеджер по Строительству, Сичим

Проверено/Рассмотрено                                                    Checked/ Reviewed

(Должность)____________________________________________ (Position):

Manas Chotong / Манас Чотонг

Sicim Technical Engineer/ Технический Инженер, Сичим

Разработано:                                                                                             Author:

(Должность)____________________________________________ (Position):

Gopal Candra Das / Гопал Сандра Дас

Sicim QA/QC Manager /  Менеджер ОК/КК, Сичим

Method  Statement for Installation of above Ground Piping

TABLE FOR CONTENTS

1.	Scope..............................................................................................................................5

2.	Abbreviations and Definitions............................................................................5

3.	Responsibilities.........................................................................................................5

4.	SUBSTANTIVE DOCUMENTATION OF HYDROTEST PACKAGE and REFERENCE DOCUMENTS..........................................................................................................................5

5.	Preliminary, Testing and Commissioning Activities...................................6

5.1.COLLECTION OF MATERIALS.................................................................................6

5.2. PIPING FABRICATION.............................................................................................6

5.3. PIPING&INSTALLATION........................................................................................6

5.4. SAFETY INDUCTION..............................................................................................7

5.5. EQUIPMENT............................................................................................................7

5.6. SITE  SURVEY........................................................................................................7

6. INSPECTION & TESTING...................................................................................................8

6.1. SHOP FABRICATION&SITE FABRICATION, INSTALLATION TESTING............8

6.2. NDT..........................................................................................................................8

6.3. DOCUMENTS (CQI&ROK) .....................................................................................8

# Scope

Contractor is responsible for Fabrication, Installation & testing for carbon Steel pipes as per approved Job pack №K3 Drain System ETP 62/15 (E/W)

# Abbreviations and Definitions

Client	      Tengizchevroil

Contractor	SICIM S.p.A.

QP	Quality Plan

ITP	Inspection & Test Plan

PM	Project Manager

CM	Construction Manager

GS	General Service /  Logistic

TO	Technical Office

QA/QC	QA/QC Engineer

QM	Quality Manager

HSE	HSE Manager

NDT              Non Destructive Testing

WPS            Welding Procedure Specification

WPQ            Welding Performance Qualification

# Responsibilities

PM is responsible for ensuring the correct implementation of the present procedure.

CM shall co-ordinate the activities with the area supervisor, who will lead the respective for fabrication, Installation & Testing Activity

QM is responsible, supported by TO, for the preparation, issuance, review, Company’s approval of all documentation, reports and site activities in accordance with the relevant specifications and with this Procedure.

# ReFERENCE

- W-ST-2000	Welding, PWHT & NDE of Piping

- L-ST-2007	Specification for Piping Installation and Testing

- ASME 31.3	Process Piping

- X-000-L-PRO-0001	Procedure for the Hydrostatic Testing of Piping Systems.

- X-ST-2000                              Paint &  Protective  Coating

# Description of activites

### 5.1. COLLECTION OF MATERIALS

Contractor Prepare Materials take it request to be made minimum 3 days before starting fabrication.

Contractor shall responsible to collect materials from TCO warehouse. As per requirement materials will be off load in fabrication shop for Pipe shop fabrication & site fabrication, installation materials will be off load in site in proper way to store to above damage & corrosion.

### 5.2.PIPE FABRICATION:

Fabrication to be done as per TCO approved WPS & WPQ & it will be monitor by    SICIM QA/QC Department.

Contractor shall ensure pre fabricated pipe spools are protected against    corrosion.

Damage or ingression of dirty/foreign matter.

Shop fabricated spool NDT to be done as per Specification & spool to be released for

Coating as per TCO Specification. Prior  to be transfer to the site for installation.

5.3.PIPING  INSTALLATION

Shop fabricated spool to be installed as per ISO drawing & TCO specification. & as per job pack №K3 Drain System ETP 62/15 (E/W)

Welding shall  be done by approved WPS & WPQ

Pipe Support shall be  installed as per ISO drawing & standard pipe Support drawing.

NDT shall be done based on line class & job pack.

Hydrostatic  test /Technical piping Passport shall be prepared.

Testing to be done as mention test pressure then reinstatement  shall be done.

All the above activities shall be monitor by SICIM QA/QC department for Quality & documentation

### 5.4. SAFETY INDUCTION

### Specific safety induction will be provided by the HSE Manager to the Personnel involved in the fabrication & installation, Testing, Discharging of Test Medium, Cleaning and Reinstatement activities, before any work is started to this extent.

Work Responsible Person must immediately stop all activities and notify Person in Charge and Facility Owner Designate in case of abnormal situations which are completely different from planned work and activities not included into the procedure.

5.5 EQUPIMENT & INSTRUMENTATION

Before starting any site operations, the area supervisor must make sure that all necessary Equipments & instruments is approved or calibrated.

The main Equipments & Instruments are the following:

Equipment:

- Welding Machine

- Crane

- Folk lift

- Air-compressor

- Filling water pump

- Pressurising pump

- Water storage tanks

Instrumentations:

- Pressure Safety Valve  (with TCO calibration certificates)

- Pressure/Temperature Recorder (with TCO calibration certificates)

- Pressure gauges (with TCO calibration certificates)

- Digital thermometer

- Temperature probes

5.6. SITE SURVEY

Before starting any site activity, the CM and HSE staff will perform an accurate site survey to define all necessary safety requirements in the working areas as well as all necessary safety signals and protections in the areas involved in the construction activities.

Client’s approval for the safety signals and protections system implemented shall be given before any site activity starts.

All water shall be filtered before introduction into the line, unless it is of potable quality and the requirement for filtering it is waived by Company. Filters shall be 50 micron mesh and shall be of capacity equal to the pipeline filing rate. Contractor shall backwash the filters or change filter elements until the backwash water meets the approval of Company.

- Test ends shall incorporate a device to establish that scrapers have arrived at the receiving end. Radioactive indicators shall not be used.

## 6.Inspection & Testing

6.1. SHOP FABRICATION&SITE FABRICATION, INSTALLATION TESTING TO BE INSPECTED BY QUALIFIED WELDING INSPECTOR FROM QA/QC DEPARTMENT

6.2. NDT TO BE DOME BY APPROVED COMPANY

6.3. SICIM QA/QC DEPARTMENT IS RESPONSIBLE FOR DOCUMENTS (CQI&ROK) AS BUILT MARK UP DRAWINGS & HAND OVER DOCUMENT.